## Slide 1: A One-Dimensional Integrated Workflow for Tungsten Sputtering, Transport, and Redeposition in the Divertor Region
Tengfei Tang，K. T. E. Chua¹ A. Geraldini² V. H. Hall-Chen¹ M. Abazorius³
¹ FEAT, A*STAR, ² University of York
³ CCFE, UKAEA
ECW 2026

## Slide 2
Tungsten impurity in Tokamak
1D Sheath model benchmark
Coupled model for the tungsten sputtering
Tungsten impurity under sheath
Summary
OUTLINE

## Slide 3
Tungsten impurity in Tokamak
Full poloidal cross-section: W source and transport path
Generation at tungsten plasma-facing components
1
Incident ions and charge-exchange neutrals strike W divertor targets.
Physical sputtering releases neutral tungsten W⁰ near the surface.
Edge plasma ionizes W⁰ to W⁺ and then higher charge states Wᶻ⁺.
Transport after ionization
What the model chain must predict
SOL/divertor
Parallel flow and friction move W ions along open field lines; many particles redeposit.
Pedestal/core
Cross-field transport, neoclassical pinch and turbulence set the inward flux.
Radiation
High-Z W radiates efficiently; small core concentration can cool and dilute the plasma.
sputtering
Y(E,θ)
ion impact
E, θ
ionization
W⁰→Wᶻ⁺
transport
SOL→core
Radiation
Core
Sheath

## Slide 4
Simulation of tungsten generation and transport
Typical code workflow for W source generation, near-wall transport, redeposition, radiation and core penetration
1 Edge plasma state
• SOLPS-ITER / EDGE2D-EIRENE
• UEDGE / Hermes-3 / SOLEDGE
• Outputs: nₑ, Tₑ, Tᵢ, Γᵢ, B, α, neutrals
2 Sheath + W source
• Analytic sheath / PIC
• SDTrimSP / TRIM / yield database
• Maps target state → IED/IAD → S_W(E,θ)
3 MC impurity transport
• ERO2.0 / DIVIMP / ASCOT/OPENEDGE/VANTAGE
• Trace W⁰ and Wᶻ⁺: ionization, CX, drifts
4 Core / MHD response
• STRAHL / JOREK / integrated models
• Pedestal-core W accumulation
• Radiative cooling, ELM/RMP/disruption effects
Sheath physics:
Floating/sheath potential sets impact energy and ion acceleration (IED)
Magnetic presheath bends gyro-orbits and changes incidence angle θ (IAD)
Near-wall full-orbit treatment controls prompt redeposition
Divertor regime changes Tₑ, Tᵢ, nₜ, Γᵢ → different W source

## Slide 5
Code workflow of the 1D model
Main coupling sequence
1. Fluid code
Hermes-3
Solve edge/divertor plasma and neutrals.
Output: n_e, T_e, T_i, Gamma_i, q_parallel, flow, B, alpha, recycling state.
2. Sheath / MPS
Clover, GYRAZE *
Map fluid target state to near-wall fields.
Output: phi_s, E(x), sheath potential, magnetic-presheath bending.
3. MC tracing
sample ions in E and B
Sample f_i(v) and integrate ion orbits.
Output: Gamma_i(E,theta), IED/IAD, flux-weighted impact distribution.
4. DSMC
near-wall W / neutrals
Track sputtered W, reflected particles and neutral collisions.
Output: redeposition, escape fraction, W source to plasma.
What each coupling stage changes
Fluid -> sheath
Plasma background
Sheath -> MC
IAE and IDE
MC -> DSMC
Sputtering yield，redeposition
*Geraldini A et al., Monotonic sheaths near a wall with grazing magnetic incidence (2025)
Wall time : minutes
tungsten atom and ion distribution at the sheath

## Slide 6
Tungsten sputtering in Tokamak
1D Sheath model benchmark
Coupled model for the tungsten sputtering
Tungsten impurity under sheath
Summary
OUTLINE

## Slide 7
Code: lizCode (based on *Smilei)
  Smilei is an open-source PIC code
Model: 1D3V
  1D in space, 3D in velocity
Particle-in-cell (PIC) sheath model: 1D3V with a plasma source
New features added:
Poisson solver: TDMA, SuperLU, MG
Code capability:
  Coloum collision; ionization; excitation; charge exchange collision; Recombination collision; sputtering yield; 2D3V; multi-species ion.
*Derouillat J et al., Comput. Phys. Commun. 222 (2018) 351-373 (Smilei PIC)
Notes: The parallel velocity of the ion is the sound speed.

## Slide 8
Calculate the GYRAZE input from the PIC input
lizCode input | 
Magnetic Field B | 2.0 T
Field Angle | 3°
Electron Temp Te | 20 eV
Ion Temp Ti | 20 eV
Plasma Density ne | 
Distribution function | Maxwellian
Target boundary | Float potential
lizCode input | 
Magnetic Field B | 2.0 T
Field Angle | 3°
Electron Temp Te | 20 eV
Ion Temp Ti | 20 eV
Plasma Density ne | 
Distribution function | Maxwellian
Target boundary | Float potential
GYRAZE Input | GYRAZE Input
Angular Parameter | 3.0°
Reference Gamma | 
Density Ratio ni/ne | 1.0
Temperature Ratio Ti/Te | 1.0
Mass Ratio mi/me | 3600
Distribution Function | Half-Maxwellian
Target boundary | 
GYRAZE Input | GYRAZE Input
Angular Parameter | 3.0°
Reference Gamma | 
Density Ratio ni/ne | 1.0
Temperature Ratio Ti/Te | 1.0
Mass Ratio mi/me | 3600
Distribution Function | Half-Maxwellian
Target boundary | 
lizCode has the bulk plasma and sheath (5 mm), no collision is added.
A drift velocity of Cs along the magnetic field line is added.

## Slide 9
Kinetic drift velocity in the PIC code: ion scale
The steady state sheath in ion time scale: :
Both the density and potential profile match the PIC result. (Clover provides a natural particle distribution at the presheath)

## Slide 10
Tungsten sputtering in Tokamak
1D Sheath model benchmark
Coupled model for the tungsten sputtering
Tungsten impurity under sheath
Summary
OUTLINE

## Slide 11
Monte-Carlo test particle code to get the IED and IAD: comparison
A new Monte-Carlo test particle code using the GYRAZE output as potential distribution to get the IED and IAD.

## Slide 12
Angle and energy distribution
With the test particle module, the final IAD and IED match the PIC results.

## Slide 13
Tungsten sputtering in Tokamak
1D Sheath model benchmark
Coupled model for the tungsten sputtering
Tungsten impurity under sheath
Summary
OUTLINE

## Slide 14
Tungsten sputtering model at the target
Eckstein formula
the code first uses Yamamura-Tawara to find the "base yield" at 0 degrees.

## Slide 15
Different method of calculation of sputtering yield
Match the PIC result.
Sheath bending used in the fluid codes get a much smaller value.
The most closed bending model should use the averaged angle from calculation.
The sheath profile from the pre sheath profile and Debye sheath profile model to get the averaged angle without direction calculations.

## Slide 16
Tungsten sputtering in Tokamak
1D Sheath model benchmark
Coupled model for the tungsten sputtering
Tungsten impurity under sheath
Summary
OUTLINE

## Slide 17
Direct Simulation Monte Carlo (DSMC) method
DSMC computational domain
target
cells Δx
sample outcoming particles
move + collide in cells
1 Initialise
Create simulation particles in each cell
from prescribed f(E,θ), density and temperature.
Each computational particle represents many physical particles.
2 Move
x(t+Δt)=x(t)+vΔt
Particles travel ballistically between collisions; external fields may be included when required.
3 Collide
P = 1 - exp(-ν Δt)
Random numbers select whether a pair collides; velocities are updated from the chosen cross section.
4 Surface
At the wall, sample reflection, sticking or sputtering from Y(E,θ).
Returned particles or sputtered atoms are inserted with sampled energy and angle.
DSMC separates particle transport into repeated move–collide–sample steps; macroscopic distributions are obtained statistically from many particle histories
Notes: DSMC method slide. This slide explains the method only: computational particles, cells, ballistic motion, stochastic collision selection, surface interactions, and tallied IED/IAD outputs. No Hermes-3, PIC, GYRAZE, or divertor-regime results are included.

## Slide 18
Tungsten generation and transport module
Monte-Carlo Ion,
DSMC neutral atom,
Kinetic sheath,
Multi-species ion source.

## Slide 19
Sputtering yield calculation: self sputtering and distribution
Distribution of the ion-W along the perpendicular direction.
Include ion-W with different charge number.
Add impurity ion W to get the self-sputtering rate.
Support different impurity ions.

## Slide 20
Redeposition rate calculation with the sheath profile
Comparing to the sheath model with similar potential drop, the redeposition rate could be largely different.
Compared to a similar analytical sheath model

## Slide 21
Summary
For the redeposition and impurity transport, a 1D neutral and impurity ion model is implemented with kinetic sheath and ionization/recombination reactions.
  The redeposition rate and self sputtering will be included.
  The impurity ion/neutral distribution could be coupled to the fluid code.
Future work:
1. The 2D sheath module.
2. Hermes-3 and VANTAGE for impurity transport.
+ INGRID